## Slide 1
M. Kopčík, V. Hašková, P. Szabó, T. Samuely, P. Samuely
Centre of Low Temperature Physics, Košice
@ Slovak Academy of Sciences & P.J.Šafárik University, Slovakia
thin film MoC samples made by
M. Grajcar and M. Žemlička
Comenius University, Bratislava, Slovakia
On the origin of the quasiparticle states in
the superconducting gap of homogeneously
disordered ultrathin films. MoC case.
Notes: Sss

## Slide 2
On the origin of the quasiparticle states in
the superconducting gap of homogeneously
disordered ultrathin films. MoC case.
Notes: Sss

## Slide 3
3D to 2D S-I transition in Bi thin films
Bosonic scenario
Fermionic scenario
Phase fluctuations of Ψ
Gradual loss of the macroscopic long range coherence
Direct transition
Amplitude fluctuations of Ψ
Gradual reduction of the order parameter Δ down to 0
Intermediary metal phase
Control parameters
Superconductor
Insulator
disorder (lattice defects, impurities)
dimensionality (3D->2D)
charge carrier concentration
external magnetic field
...
Superconductor-Insulator Transition
Superconductivity
macroscopic wave function

## Slide 4
prepared by the reactive magnetron sputtering
on single-crystal sapphire substrates ( at 200 oC)
in a mixture of Ar and acetylene gas
t = 10 nm Rs (10 K) = 344 W, Tc = 6.7 K, kFl = 2
t = 5 nm Rs (10 K) = 850 W, Tc = 3.3 K, kFl = 1.8
t = 3 nm Rs (10 K) = 1227W, Tc = 1.3 K, kFl = 1.3
Thin films of MoC
Cubic B1 lattice
STM scans reveal the (111) plane with lattice constant a0 = 0.42 nm

## Slide 5
10 nm 5 nm 3 nm
G/D = 0.1 D , Tc = 6.5 K,
2D/kBTc = 3.85
G/D = 0.3 D , Tc = 3.5 K,
2D/kBTc = 3.87
G/D = 0.9 D , Tc = 1.35 K,
2D/kBTc = 3.7-4
Fitting to
Dynes DOS:

## Slide 6
Bosonic insulator scenario:
Tc and D decrease
2 D / kBTc increase
D inhomogeneity on scale of x
pseudogap appearance
Fermionic scenario:
Tc and D decrease together
2D / kBTc almost not changing
No D fluctuations
no pseudogap
the bosonic picture is not universal
Fermionic SIT in MoC
[1] P. Szabó, et al., Phys. Rev. B 93, 014505 (2016).
[2] M. Žemlička, et al., Phys. Rev. B 92, 224506 (2015.)
increased disorder – increased spectral smearing - increase of in-gap states disorder leads to pair-breaking or interface effect (new theory?)

## Slide 7
Finite lifetime effect (Dynes formula):
Parameter G can account for broadening if necessary
via substitution of complex E’ = E- iG instead of E in NSBCS
Fermionic SIT in MoC

## Slide 8
Smeared tunnelling spectra in disordered thin films
Fitting to Dynes formula

## Slide 9
DOS – pair-breaking, disorder
K. Maki
Prog. Teor. Phys. (Kyoto) 29, 333 (1963)
P. G. de Gennes
Phys. Kondens. Materie 3, 79 (1964)
S. Skalski, O. Betbeder-Matibet a P. R. Weis
Phys. Rev. 136, A1500 (1964)
Universal pair – breaking model
Disorder with strong Coulomb interaction
Gapless superconductivity near
the critical pair breaking
M. Feigel’man, M. Skvortsov
Phys. Rev. Lett. 109, 147002 (1963)
The local pairing field fluctuates in the space
smearing the BCS coherence peak
subgap tail states

## Slide 10
Lorentzian distribution of the pair-breaking potential V, width of the distribution G
microscopic interpretation of the phenomenological Dynes model
PHYSICAL REVIEW B 94, 144508 (2016)
Microscopic interpretation of the Dynes formula for the tunneling density of states
Validating this model –same film thickness + different substrates

## Slide 11
Aký je pôvod nárastu rozmazania?
MoC / Al2O3
MoC / Si
MoC -3 nm films sputtered
simultaneously on different substrates:
c-cut saphire (Al2O3)
silicon (Si)
MoC/Si: Tc = 3.5 K
MoC/Al2O3: Tc = 2.5 K
RN = 1120 Ω
MoC / Al2O3, MoC / Si – 3 nm thin films
surface corrugation 0.7 nm

## Slide 12
Aký je pôvod nárastu rozmazania?
MoC / Al2O3
MoC / Si
MoC -3 nm films sputtered
Simultaneously to different substrates:
c-cut saphire (Al2O3)
(100) silicon (Si)
MoC/Si: Tc = 3.5 K
MoC/Al2O3: Tc = 2.5 K
RN = 1120 Ω
MoC / Al2O3, MoC / Si – 3 nm thin films
MoC thin films of the same thickness - DIFFERENT SUBSTRATES - DIFFERENT TC
DIFFERENT PHASES? SAMPLE INHOMOGENEITY?

## Slide 13
MoC / Al2O3, MoC / Si – 3 nm thin films
MoC / Al2O3
MoC / Si
MoC -3 nm films sputtered
Simultaneously to different substrates:
c-cut saphire (Al2O3)
silicon (Si)
MoC/Si: Tc = 3.5 K
MoC/Al2O3: Tc = 2.5 K
RN = 1120 Ω
CITS studies – I-V measurements in 128 x 128 points of topography - homogeneous superconductivity

## Slide 14
ΔSi = 0.66 meV
wSi = 0.09 meV
ΔAl2O3 = 0.5 meV
wAl2O3 = 0.1 meV
ΓSi = 0.2 meV
uSi = 0.089 meV
Γ Al2O3 = 0.225 meV
uAl2O3 = 0.11 meV
MoC / Al2O3
MoC / Si
CITS – I-V measurements in 128 x 128 points of the topography
Fitting of 16384 I-V curves to Dynes formula
Statistical distribution of D and G values:

## Slide 15
MoC / Al2O3
MoC / Si
Fitting of 16384 I-V curves to Dynes formula
Statistical distribution of D and G values:
CITS – I-V measurements in 128 x 128 points of the topography

## Slide 16
ΔSi = 0.66 meV
wSi = 0.09 meV
ΔAl2O3 = 0.5 meV
wAl2O3 = 0.1 meV
ΓSi = 0.2 meV
uSi = 0.089 meV
Γ Al2O3 = 0.225 meV
uAl2O3 = 0.11 meV
MoC / Al2O3
MoC / Si
Fitting of 16384 I-V curves to Dynes formula
Statistical distribution of D and G values:
ΔSi > ΔAl2O3 and GSi < GAl2O3 due to different pair breaking
in different substrates?
if yes – thickness dependent pair-breaking
rough surfaces
CITS – I-V measurements in 128 x 128 points of the topography

## Slide 17
CITS - ROUGH surfaces:
The peak-VOLTAGE position map fits the surface
Peak-position map at 0.5 K
Topography at 0.5 K
small cca. 10% variation of D observed in thicker areas with corrugation ~ 1 nm
MoC / Al2O3
MoC / Si
0 nm
1.7 nm
0.7 mV
0.9 mV
2 nm
0 nm
1.1 mV
0.85 mV
How local D correlates with G ? - increase resolution

## Slide 18
MoC / Si
0 nm
2 nm
Zoom – protruding boomerang:
CITS + Fitting of 16384 I-V curves to Dynes formula
CITS – I-V measurements in 128 x 128 points of the topography

## Slide 19
MoC / Si
0 nm
2 nm
Zoom – protruding boomerang:
CITS + Fitting of 16384 I-V curves to Dynes formula
Topography vs. Gap-map vs. Gamma-map:
CITS – I-V measurements in 128 x 128 points of the topography

## Slide 20
MoC / Si
0 nm
2 nm
Zoom – protruding boomerang:
CITS + Fitting of 16384 I-V curves to Dynes formula
Topography vs. Gap-map vs. Gamma-map:
CITS – I-V measurements in 128 x 128 points of the topography

## Slide 21
MoC / Si
0 nm
2 nm
Zoom – protruding boomerang:
CITS + Fitting of 16384 I-V curves to Dynes formula
Topography vs. Gap-map vs. Gamma-map:
Thinner sample – smaller gap D – higher Gsmearing – the interface is the source of pair-breaking
CITS – I-V measurements in 128 x 128 points of the topography

## Slide 22
Aký je pôvod nárastu rozmazania?
CONCLUSIONS
MoC / Al2O3
MoC / Si
films prepared simultaneously on Al2O3 and Si substrate:
MoC
- Interface induced pair-breaking, proposed by Herman and Hlubina
- Equal sheet resistance
different Tc
(equal disorder)
- Lowering the thickness in MoC/Al2O3 and MoC/Si -
suppressed D + increased G
MoC / Al2O3
MoC / Si
superconductivity is suppressed near the substrate
samples with the same disorder differ only in the substrate
– the source of pair breaking - interface
source of pair breaking – uncompensated electron orbitals at the inteface?

## Slide 23
On the origin of the quasiparticle states in
the superconducting gap of homogeneously
disordered ultrathin films. MoC case.
Progress in Applied Surface, Interface and Thin Film Science 2017
International Conference on Multi-Condensate Superconductivity and Superfluidity in Solids and Ultra-cold Gases
International Workshop on the Superconductor-Insulator Transition and Low-Dimensional Superconductors
Firenze, 20-23.11.2017
Villard de Lans, 7-12.10.2018
Trieste, 14-18.5.2018
Notes: Sss

## Slide 24
Thank you for your attention