## Slide 1
Súťaž mladých
RNDr. Jozefína Majorošová
Košice 2016
Adsorpcia magnetitu na amyloidných fibrilách

## Slide 2: Lyotropic liquid crystal
Suitable concentration and temperature LLC phase
Main components:
amphiphilic molecules and solvent

## Slide 3: Motivation
Center of our interest: Liquid Crystals (LC) doped with magnetic nanoparticles
Corrigan et al., Jacs Communications 2006:
preformed amyloid fibrils of hen lysozyme (LAF) can form liquid crystal phases
J.J. Vallooran et al. Advanced Materials 23, 3932 (2011) :
usage of magnetic particles can facilitate lyotropic LC alignment
M. Zaman et al. International Journal of Nanomedicine, 9 (2014), 899-912 :
some minimal (critical) concentration (cc) exists at which the amyloid fibrils order to pure biological LC
Aim: explore the interactions of biological LC with magnetic nanoparticles
Schematic picture of LAFdoped with MNPs

## Slide 4: Experiment
There is opportunity to further fibrils ordering into the liquid crystal phase by applying external magnetic field.
Lysozyme from Hen egg white
Aim:
Order fibrils under cc using
MNP and external magnetic field.
c<cc
Interaction of MNPs
with LAF
Mezophase of biological LC.

## Slide 5: Results: TEM
Magnetic fluid
Lysozyme amyloid fibrils LAF
Mixture of MNPs and LAF:
cMNP =0.5 mg/mL cMNP =2.5 mg/mL cMNP = 5 mg/mL
The measurenments: in cooperation with co-authors from Faculty of Physics, Adam Mickiewicz University, Poznań, Poland

## Slide 6: Results: SAXS
The measurenments: in cooperation with co-authors from Hamburg, Helmholtz-Zentrum Geesthacht, Germany
Effect of MNPs concentration
Od cMNP =2,5mg/ml alongated asocciations
Nativ protein

## Slide 7: Results: SAXS
The measurenments: in cooperation with co-authors from Hamburg, Helmholtz-Zentrum Geesthacht, Germany
Cross-section pair distribution function
Radial contrast of scattering length density profile

## Slide 8: Results: Faraday rotation
The measurenments: in cooperation with co-authors from Faculty of Physics, Adam Mickiewicz University, Poznań, Poland
Fe3O4 concentration | Fe3O4 Volume fraction | Saturation FR [◦ mL/mg m] | Vsp [◦ mL/m T mg]
0,5 | 1 × 10−4 | −59 ± 4 | −271 ± 84
2,5 | 5 × 10−4 | −64 ± 1 | −571 ± 51
5 | 1 × 10−3 | −70 ± 1 | −771 ± 54

## Slide 9: Summary
J. Majorošová et al. Col. Surf. B (2016).
syntetized biohybrid
Adsorbtion of MNP on LAF
Critical concentration
ability to further fibrils ordering into the LCphase by applying external magnetic field.

## Slide 10: Acknowledgement
doc. RNDr. Peter Kopčanský, CSc.
RNDr. Natália Tomašovičová, CSc.
RNDr. Zuzana Gažová, PhD.
RNDr. Katarína Šipošová PhD.
RNDr. Milan Timko, CSc.
PhD. Vasil M. Garamus
Dr. Viktor I. Petrenko
Dr. Mikhail V. Avdeev
PhD. Marceli Koralewský
Dr. Błażej Leszczynski
Dr. Stanislaw Jurga
Dr. Chin-Kun Hu
Dr. Shura Hayryan

## Slide 11
Thank you for attention !

## Slide 12
AFM
1μm
100 nm
100 nm
Clyzosyme= 10mg/ml

## Slide 13: AFM
The measurenments: in cooperation with M. Baťková, IEP SAS Košice

## Slide 14: Future plans
Data processing from SAXS and SANS
Order lysozyme amyloid fibrils in magnetic field to prepare lyotropic liquid crystal SANS Budapešť, SANS (Grenoble)
Study the interaction of LAF with nanoparticles of different shapes.
Doping the lysozyme amyloid fibrils with spindle nanoparticles